## Slide 1
Explainable & Uncertainty-Aware Machine Learning for LPBF Ti-6Al-4V
Predicting Porosity and Mechanical Properties using Process–Structure–Property Features
1
PROJECT BY: -
G. Subhash Guptha(23015)
R. Gautam(23022)
K. Mithul(23025)
S.V. Sai Sashank(23043)
SUBMITTED TO:-
Dr. Sathies T

## Slide 2
Literature Review
Selected paper and the experimental foundation for our project
Selected Paper
Luo et al. (2023) “Dataset of process-structure-property feature relationship for laser powder bed fusion additive manufactured Ti-6Al-4V material” Data in Brief, 46, 108911 The dataset links LPBF processing conditions with pore structure, grain morphology, surface roughness and mechanical properties.
What the paper studied
42 unique combinations of laser power and scan speed using LPBF Ti-6Al-4V.
How it was characterized
XCT + image analysis for pores; optical microscopy for grains; tensile testing and Vickers microhardness for properties.
What it enables
A quantitative process–structure–property dataset suitable for ML development, analysis and process optimization.
2

## Slide 3
Literature Review
What the dataset provides: process, structure and property features
PROCESS
Laser power Scan speed Linear energy density Modified energy-density descriptor P × v Hatch spacing and layer thickness were fixed in the campaign.
STRUCTURE / DEFECTS
Archimedes & XCT porosity Pore quantity Pore size Pore sphericity Projected pore area Surface roughness Prior-β grain size & aspect ratio
PROPERTIES
Yield strength Ultimate tensile strength Elongation to necking Elongation to fracture Young’s modulus Vickers microhardness
3

## Slide 4
Motivation
Why this project is needed
Manufacturing motivation
LPBF Ti-6Al-4V has nonlinear relationships between process parameters, defects, microstructure and final properties. Experimental trial-and-error is costly and time-consuming.
Machine-learning motivation
ML can reduce repeated experiments, but small and correlated datasets can produce unreliable or overly optimistic results if validation is not designed carefully.
WE NEED TO PREDICT
Porosity Strength Ductility Hardness / modulus
WE NEED TO EXPLAIN
Which process, pore and grain features contribute to predictions?
WE NEED TO TRUST
How certain is the prediction and is it inside the supported process range?
4

## Slide 5
Problem Statement
The central research problem
CURRENT SITUATION
LPBF Ti-6Al-4V produces complex relationships among process parameters, porosity, microstructure and mechanical properties.
LIMITATION
Simple ML comparisons may report accuracy without addressing data leakage, feature-group value, prediction uncertainty or extrapolation.
RESEARCH PROBLEM
How can we build a reliable and explainable ML framework that predicts porosity and mechanical properties while quantifying feature contributions and prediction uncertainty, using only experimentally supported process conditions?
5

## Slide 6
Objectives
DATA
Clean standardized dataset + data dictionary
EDA
Distribution, correlation, process-map and relationship plots
ML
Model performance comparison for selected targets
EXPLAINABILITY
SHAP / feature-importance / ablation plots
UNCERTAINTY
Prediction intervals + high-uncertainty regions
OPTIMIZATION
Constrained Pareto-front / promising process conditions
REPORT
Reproducible Python code + final project report
6

## Slide 7
Availability of the Datasets
Public data used as the foundation of the project
DATASET SOURCE
Zenodo — record 6587905 The paper states that the processed feature table and raw experimental data are publicly available.
WHAT IS AVAILABLE
Processing features, porosity, pore morphology, surface roughness, grain morphology, mechanical properties, hardness and supporting raw experimental files.
42 CONDITIONS
Unique combinations of laser power and scan speed.
PUBLIC ACCESS
The paper reports no specific access restrictions for the repository.
PROJECT USE
Start with the processed feature table; raw microscopy images and complete stress–strain curves are outside the first implementation scope.
7

## Slide 8
Methodology: Workflow
Only the project workflow needed to explain how the research will be carried out
1. Dataset audit
Units, missing values, repeated measurements, feature definitions
2. Feature groups
Process-only → process + defect → full PSP
3. EDA
Distributions, correlations, process maps, porosity/property relationships
4. ML models
Ridge, SVR, Random Forest, XGBoost, Gaussian Process, PyTorch MLP
5. Validation
Grouped 5-fold CV by laser power, compared with random CV
6. Explainability
SHAP, permutation importance, PDP/ICE, ablation
7. Uncertainty
Prediction spread, ensembles, GPR, conformal/interval methods
8. Optimization
Constrained search + Pareto-front analysis
8

## Slide 9
Methodology: Steps
What the project will accomplish
1
Collect, clean and standardize the publicly available Ti-6Al-4V PSP dataset.
2
Explore relationships between process parameters, porosity, pore morphology, grain morphology and mechanical properties.
3
Develop baseline regression models for porosity and key mechanical properties.
4
Compare process-only, defect-only/combined and full PSP feature groups.
5
Evaluate models with cross-validation grouped by laser power.
6
Apply explainability methods to identify influential features.
7
Estimate prediction uncertainty using suitable ensemble, Gaussian-process or interval methods.
8
Develop constrained multi-objective optimization within the experimental process range.
9

## Slide 10
Methodology Focus: Grouped Validation
A key part of the proposed research
RISK WITH RANDOM SPLITTING
Many conditions share the same laser power. A random split leaves close neighbours of each test point in training, so scores may not reflect a genuinely new power level.
PROPOSED SOLUTION
Put all conditions with the same laser power in one fold (GroupKFold), so every test fold holds unseen power levels.
VALIDATION
Grouped 5-fold CV (groups = laser power) Random 5-fold CV, 10 seeds for comparison
METRICS
MAE RMSE R² Prediction-interval coverage
ROBUSTNESS
Compare random vs grouped splitting Assess fold-to-fold variation
10

## Slide 11
Results: Validation and Model Benchmark
35 XCT conditions, 6 models, 3 feature groups, GroupKFold by laser power
11
Key numbers (grouped CV)
• P and v only: R² = 0.65 UTS, 0.71 yield, 0.81 elongation
• Adding pore features: UTS 0.68, yield 0.74; elongation drops to 0.64
• Porosity from P and v: best R² = -0.06, not predictable
• Hardness: best R² = 0.14; spread between conditions (12.7 HV) is below indent scatter (19.1 HV)
• Random vs grouped CV: random scored higher for only 1 of 6 models on UTS, so no consistent optimism here

## Slide 12
Results: Explainability and Uncertainty
SHAP on XGBoost (UTS, 15 features); intervals from held-out power groups
12
What the numbers say
• XCT porosity is the largest SHAP contributor (mean |SHAP| 21 MPa, down to -85 MPa for the most porous set); higher LED lowers predicted UTS
• Gaussian process 95 % band covers 90 % of held-out conditions; MC dropout only 81 % (too narrow)
• Cross-conformal: 95 % coverage at the 90 % level, but intervals ≈ 118 MPa wide

## Slide 13
Results: Process Search and Data Check
Pareto search for min porosity, max UTS, max elongation inside the tested region
13
Findings
• Pareto set: P = 230–275 W, v = 1080–1460 mm/s, LED = 188–223 J/m
• Contains measured set 41 (235 W, 1200 mm/s): UTS 1113 MPa, elongation 15.38 %, porosity 0.0132 %
• Suggestions confirm the measured best region; they must be built and tested before use
• Data check: the printed Table 8 headers swap yield strength and UTS; corrected using the Zenodo files

## Slide 14
Project Takeaway
What we found
DATASET
42 LPBF conditions
QUESTION
Can we predict reliably?
METHOD
ML + grouped validation
TRUST
Explainability + uncertainty
OUTPUT
Constrained optimization
Main message
Laser power and scan speed alone predict strength and ductility at unseen power levels (grouped R² 0.65–0.81); pore and grain features add little. Porosity and hardness could not be predicted. Uncertainty is quantified, and the process search, kept inside the tested region, points to 230–275 W and 1080–1460 mm/s, where the best measured specimen lies.
14

## Slide 15
References
Luo, Q., Yin, L., Simpson, T. W., & Beese, A. M. (2023) — Dataset of process-structure-property feature relationship for laser powder bed fusion additive manufactured Ti-6Al-4V material.
Data in Brief, Volume 46, Article 108911 — selected as the main experimental dataset/reference for this project.
Luo, Q., Yin, L., Simpson, T. W., & Beese, A. M. (2022) — Effect of processing parameters on pore structures, grain features, and mechanical properties in Ti-6Al-4V by laser powder bed fusion.
Additive Manufacturing (2022) — used to understand relationships between LPBF processing parameters, pore structures, grain features and mechanical properties.
Zenodo Dataset — Record 6587905 — public dataset containing the processed feature table and supporting experimental data.
The Luo et al. papers and the Zenodo files are the technical sources for all data used here.
15